## Slide 1
Welcome FuseNet@ITER
Tritium Breeding Technologies and the TBM Program
 Preparing the NEXT STEP after ITER

## Slide 2: FuseNet@ITER, 181107-9
Outline
Fusion Electricity - next steps after ITER
Tritium Breeding Blankets
Test Blanket Modules Program in ITER
Disclaimer:
The views and opinions expressed today do not necessarily reflect those of the ITER Organization or the ITER Members

## Slide 4
ITER
China EU India Japan Korea Russia USA
Global challenge, global response

## Slide 5
ITER
500 MWth

## Slide 6
Picture from French Embassy website
Hinkley Point C
2 x 4524 MWth
2 x 1630 MWe

## Slide 7: ITER Site 2025
tokamak complex

## Slide 8
Fusion Electricity: bringing time forward

## Slide 9
Power Plant Breeding Blanket functions
Three crucial functions:
Convert the neutron energy (80% of the fusion energy) into heat and collect it by mean of an high grade coolant to reach high conversion efficiency (>30%)
In-pile heat exchanger
Produce and recover all Tritium required as fuel for D-T reactors
Tritium breeding self-sufficiency
Contribute to radiation shielding of the superconducting coils
 Resistant to high neutron flux and fluence
See talk by R. Raffray

## Slide 10
Typical Tritium production rate in heavy water reactor : 1-2 kg T / GWth / y
Typical Tritium burn rate in a fusion reactor : ~ 70 kg T / GWth / fpy (~150 gT/GWth/day)
Need to produce all Tritium and collect it on-line (because of initial inventory and safety)
Tritium Breeding Ratio, TBR = Tproduced / Tburnt > 1 (at least)
Breeding blankets: Tritium Breeding Self-sufficiency
Tritium breeding self-sufficiency : a necessity
Tritium breeding self-sufficiency : a severe constraint
20 to 40 % of neutrons
are not available for
T-production
Neutron Losses
n-leakage through ports,
divertor region, gaps
 10 – 20 %
n-parasitic absorptions on other materials (structures)
 10 – 15 %
blanket n-leakage (< 5%)
Neutronics requirements
minimize n-losses
 small gaps and openings,
minimization of structures
and coolant fractions
add a n-multiplier
 Pb (n, 2n) or Be (n,2n)
or 7Li (n, n’T)
Main Tritium production reaction : 6Li + n => T + 4He + 4,8 MeV

## Slide 11: Deuterium-Tritium Fuel Cycle (2/2)
Ingredients for fusion energy systems with Tritium self-sufficiency: add 6Li as close as possible around the plasma to capture neutrons*
Main available T-breeders (Li-based compounds):
Solid Li-Ceramics: Li2O, Li4SiO4, Li2TiO3
Liquid Lithium (natural 7.5% 6Li)
Liquid Eutectic Pb16Li-alloy (Tmelting: ~ 235°C)
Liquid Molten Salts : FLiBe, FLiNaBe
Neutron multipliers:
Be (n, 2n)
Pb (n, 2n)
7Li (n, n’T)
Main Structural Materials (BlanketModules)
Ferritic/Martensitic Steels
Vanadium Alloys
Composites SiC/SiC
Main Coolants (relevant for plant efficiency)
Pressurized Water (LWR, SCWR)
Gas: Helium, CO2)
Liquid Metals: Li, LiPb-alloy
* In Blue Bold: covered by present ITER TBM Program

## Slide 12
Breeding Blanket Nuclear Design

## Slide 13: Material challenges for Gen4 & Fusion
ITER
AGR
[Based on Zinkle, SMINS, 2007]
DEMO/FPR divertor (consumable)

## Slide 14: Reduced Activation Ferritic-Martensitic Steels (1/2)
Belongs to the series of 9%Cr F/M Steels used in the tempered martensite microstructure
Reduced Activation:
  Low level waste already after 80-100 years
  Nb and Mo are dominating
Long term irradiation of a DEMO First Wall: 12.5MWa/m2: ~115 dpa
R. Lindau et al., Fusion Eng. and Design 75-79 (2005) 989-996

## Slide 15: Reduced Activation Ferritic-Martensitic Steels (2/2)
RAFM Steel compositions presently considered (TBM CD inputs)
 | EU HCLL & HCPB |  | JA WCCB | KO HHCR | CN HCCB |  | IN LLCB
Elements / wt% | GradeX10CrWVTa9-1 (Eurofer97) as in RCC-MRx 2012 | GradeX10CrWVTa9-1 (Aimed for values) | F82H [Target] | ARAA | CLF-1 | CLAM | IN-RAFMS
Ag |  |  |  |  |  | <0.005 | 
Al | < 0.0100 | As low as possible | < 0.1 | ≤ 0.1 | <0.03 | <0.01 | 0.005
As |  |  |  |  |  | <0.005 | 0.01
As+Sn+Sb |  |  |  | ≤ 0.05 |  |  | 
As+Sn+Sb+Zr |  | < 0.05 |  |  | <0.005 |  | 
B | < 0.002 | As low as possible | <0.003 [0.0010] | < 0.002 | <0.005 | <0.002 | 0.001
C | 0.09 to 0.12 | 0.11 | 0.08-0.12 [0.10] | 0.080 – 0.12 | 0.11±0.015 | 0.1±0.02 | 0.12
Co | < 0.0100 | As low as possible | < 0.01 | ≤ 0.1 | <0.01 | <0.01 | 0.005
Cr | 8.5 to 9.5 | 9 | 7.5-8.5 [8.0] | 8.70 – 9.300 | 8.5±0.3 | 9.0±0.5 | 9.2
Cu | < 0.0100 | < 0.0050 | < 0.05 | ≤ 0.1 | <0.01 | <0.01 | 0.002
Fe |  |  |  |  |  |  | 88.1
H |  |  |  | ≤ 0.01 |  |  | 
Mn | 0.20 to 0.60 | 0.40 | 0.05-0.5 [0.45] | 0.30 – 0.60 | 0.5±0.2 | 0.45±0.2 | 0.6
Mo | < 0.0050 | As low as possible | < 0.05 | ≤ 0.05 | <0.01 | <0.005 | 0.002
N | 0.015 – 0.045 | 0.03 | < 0.002 | 0.005 – 0.015 | 0.02-0.035 | <0.02 | 0.04
Nb | < 0.0050 | As low as possible | < 0.1 | ≤ 0.05 | <0.01 | <0.005 | 0.001
Ni | < 0.1 | < 0.0050 |  | ≤ 0.1 | <0.01 | <0.01 | 0.005
O | < 0.01 |  | < 0.005 | ≤ 0.1 | <0.005 | <0.01 | 0.01
P | < 0.005 | - | < 0.01 | ≤ 0.05 | <0.005 | <0.005 | 0.002
S | ≤ 0.005 | - | < 0.01 | ≤ 0.05 | <0.005 | <0.005 | 0.002
Sb |  |  |  |  |  | <0.005 | 0.01
Si | < 0.050 | - | < 0.2 | 0.05 – 0.15 | <0.05 | <0.05 | 0.05
Sn |  |  | < 0.004 |  |  | <0.005 | 0.01
Ta | 0.10 – 0.14 |  | 0.01 - 0.1 [0.08] | 0.005 – 0.09 | 0.10±0.03 | 0.15±0.02 | 0.08
Ti | < 0.02 |  | < 0.01 | 0.005 – 0.020 | <0.01 | <0.01 | 0.005
V | 0.15 – 0.25 |  | 0.15-0.25 [0.20] | 0.05 – 0.30 | 0.3±0.1 | 0.2±0.05 | 0.24
W | 1.0 – 1.2 | 1.1 | 1.8-2.2 [2.0] | 1.00 – 1.40 | 1.5±0.2 | 1.5±0.1 | 1.5
Zr |  |  |  | 0.005-0.020 |  |  | 

## Slide 16: Lithium-ceramics and Beryllium Pebble-Beds
Ceramic Breeder: Ternary Lithium Oxides, based on Li4SiO4 and Li2TiO3
T-production rate be raised by enrichment in 6Li (typically 30–60%).
Neutron multiplier: beryllium, beryllium alloys
Technology chosen for pebble production aims at low long term activation and the possibility to recycle (dissolution or remelting) of all the materials
Pebble-beds purged with He+H2 gas for T-extraction
Li2TiO3
Be

## Slide 17: Pb16Li – Lithium Lead eutectic alloy
Pb16Li has melting point at about 235 °C
Always applied as a loop
Tritium extraction is performed outside the VV
6Li can be added in the loop
taken from: I. Ricapito et al. / Fusion Engineering and Design 89 (2014) 1469–1475

## Slide 18
Testing of Tritium Breeding Blankets in ITER
Oone of the ITER missions is the following (cf. Project Specifications): “ITER should test tritium breeding module concepts that would lead in a future reactor to tritium self-sufficiency, the extraction of high grade heat and electricity production.”
All IO-CT & DA activities related to this mission form the “TBM Program”

## Slide 19: Scheme of a Test Blanket System
Example of the HCLL TBS - Locations in the various ITER buildings

## Slide 20
Overall View of the 6 Test Blanket Systems in the Tokamak Complex

## Slide 21
View of the 6 Test Blanket Module Designs
EU-HCLL
EU-HCPB
JA-WCCB
KO-HCCR
IN-LLCB
CN-HCCB
Helium coolant:
80 bar
300 – 550°C
Water coolant:
155 bar
280 – 325 °C

## Slide 22
Main Objectives of the TBM Program
Validation of the nuclear response prediction with existing modelling codes and nuclear data
Assessment of the TBMs thermo-mechanical behaviour at relevant temperature and volume heat sources using the specifically developed structural materials
Demonstration of the tritium management, including validation of Tritium extraction techniques and permeation reduction capability; validation of modelling for extrapolation to DEMO
Breeding Blanket performance for an extended period of time in order to obtain initial reliability data
Post-Irradiation Examinations for material/process data

## Slide 23
The operation of the TBS must not jeopardize ITER performance, reliability / availability and safety  the TBM testing plan has to be adapted to the ITER operation plan
Up to 4 design versions per each TBM will be tested in order to take into account the various ITER operation conditions
 the TBM Port Plugs have to be replaced ~3 times
TBM Program Testing Plan - Adopted Strategy
Typical TBS testing sequence:
TBS learning/validation phase
the Electro Magnetic version (EM-TBM): during the initial H phase and H-He phase
the Thermal/Neutronic version (TN-TBM): during D & initial DT1 phase (low duty)
TBS data acquisition phase
the Neutronic/Tritium & Thermo-Mechanic version (NT/TM-TBM): during final DT1 phase (low duty)
the INTegral TBM (INT-TBM): during DT2 phase (high duty, long pulses)

## Slide 24: ITER Research Plan & associated TBM Program

## Slide 25
Fusion Electricity: bringing time forward

## Slide 27
Reactors | JET, TFTR, JT60, Tore Supra Asdex, etc. | one ITER | DEMOs | FOAK Commercial Power Plants
Main | Plasma Physics (control,stability, impurities, shutdown proc., heating, etc.) | Plasma Q=10 Long D-T pulses Systems Integration | Tritium Breeding Self-sufficiency High Safety Standards | Electricity Production at Competitive Cost High Reliability
Goals | Magnetic Field Advanced Systems (e.g., super cond. coils) | Test of DEMO Blanket Mock-ups (Test Module) | Electricity Production (high efficiency, but limited availability) | High Availability Low Level Waste
Operation Years | Since 1980 | ~ 2030 - 2050 | > 2050 ? | > 2070 ?
Breeding Blankets Development Timescale

## Slide 28
ITER
China EU India Japan Korea Russia USA
Global challenge, global response

## Slide 29
ITER
China EU India Japan Korea Russia USA
Global challenge, global response

## Slide 30
Additional Slides

## Slide 31: ITER Fuel Cycle
Tritium is a pure β-emitter (Emax = 18 keV)
Half life t1/2 = 12.323 years
1 gram T = 324 mW decay heat
Main radiological hazard through ingestion
Plasma T throughput ~ 1 kg/hr
Plasma T inventory ~ 0.2 g
T inventory on-site < 4 kg
Fuel cycle inventory ~ 2 kg
ITER Fueling systems:
Gas Injection
Solid Pellet Injection
Neutral Beam Injection
The ITER Tritium–plant is a 7-floor nuclear building: H 35, L 80, W 25 m

## Slide 32
ITER
800 m3
~ 500 MW th
DEMO, pre-industrial demonstrator
~ 500 Mwe, 1 200 MW th,
ITER and beyond

## Slide 33: Of bathtubs and laptop batteries…
+
Lithium* contained in the battery of a single laptop computer and deuterium from half a bathtub of water can provide 200,000 kilowatt/hours of electricity.
That's enough to cover for 30 years the energy needs of one person in Western Europe.
* Neutrons impacting Lithium generate Tritium

## Slide 34
ITER
China EU India Japan Korea Russia USA
Global challenge, global response

## Slide 35
ITER
China EU India Japan Korea Russia USA
Global challenge, global response