## Slide 1
Plasma Meets Wall
Steven Lisgo1
G. De Temmerman1 (knowledge diffusion)
engineering support:
F. Escourbiac1, T. Hirai1, R. Mitteau2
1ITER CT, 2CEA/IRFM
FuseNet PhD Event, Provence 6-8/11/2018
The views and opinions expressed herein do not necessarily reflect
those of the ITER Organization

## Slide 2
…
Overview
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY

## Slide 3
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Perspective – The importance of a balanced Inside/Outside-View
[Delusion and Deception in Large Infrastructure Projects, Flyvberg et al.]

## Slide 4
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The Fusion Wheel of Pain – All aspects must be fully addressed
[EPRI Report, 1994, short]

## Slide 5
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Physics – Pretty cool

## Slide 6
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Engineering – A craft, and the burden of being real life
Fusion research can probably learn from systems engineering.
[GFI]
[The Iron Ring]

## Slide 7
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Sociology – A big challenge
For me, the sociology is harder than the physics.

## Slide 8
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The challenge of complexity
“ We can not solve our problems with the same level of thinking that created them. ” – Einstein
Complex problems need to be solved on many levels at the same time.

## Slide 9
…
Overview
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY

## Slide 10
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
ITER Plasma Facing Components (PFCs), vacuum vessel

## Slide 11
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
ITER Plasma Facing Components (PFCs), water manifolds

## Slide 12
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
ITER Plasma Facing Components (PFCs), shield blocks

## Slide 13
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
ITER Plasma Facing Components (PFCs), First Wall Panels (FWPs)

## Slide 14
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
ITER Plasma Facing Components (PFCs), The Divertor

## Slide 15
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The Divertor
100 MW
-70%
BODY (EU)
INNER
VERTICAL TARGET, IVT (EU)
OUTER
VERTICAL TARGET, OVT (JA)
DOME
(RF)
For the engineering design, a 5 mm radial exponential decay length at the outer mid-plane was assumed for the power channel.

## Slide 16
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The Divertor
B
E
…
– Plasma detachment

## Slide 17
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The Divertor – Active cooling

## Slide 18
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The Divertor – Plasma Facing Units (PFUs) and mono-blocks
!
TUNGSTEN MONO-BLOCKS

## Slide 19
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The Divertor – Plasma Facing Units (PFUs) and mono-blocks
Inventing as we go – many systems have had development issues.
Only happening for the highest heat-flux specification of 20 MW m-2 for 10 seconds.
“ITER turbulence.” – A. Kukushkin

## Slide 20
EDDY SIMULATIONS
[O. Aybay, Fluid Mechanics and Multidisciplinary Design, 2010]
FLOW
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
The Dome
W FLAT TILE ARMOUR
HYPER-VAPOTRON

## Slide 21
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
First Wall Panels (FWPs)
BERYLLIUM TILES

## Slide 22
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
First Wall Panels (FWPs) – Mock-ups

## Slide 23
…
Overview
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY

## Slide 24
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Plasma fluence in high duty-cycle devices
Start the pulse… and go for a coffee.
One morning of ITER operation = three decades of JET, in terms of plasma to surfaces.

## Slide 25
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
R.A.M.I. – Engineering considerations for high duty-cycle
Reliability. Accessibility. Maintainability. Inspectability.

## Slide 26
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Discrete tiles and leading edges
Small tiles lower thermal stress, but give many edges that can initiate cascade failure.
ELM ION
MELTING IN
ITER?
[J. Gunn]
ALCATOR C-MOD
[B. Lipschultz]

## Slide 27
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor divertor – Large modular components
In ITER, the entire cassette is thrown away if the strike-point surface is damaged.
Replacement time: 6-9 months, which is impractical for a power plant.

## Slide 28
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Photon dissipation
Strong impurity seeding: 95% of the power escaping the core is radiated (70% in ITER).

## Slide 29
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Photon dissipation

## Slide 30
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Photon dissipation
“Confinement predictions for DEMO under these conditions require future work.”
[Kallenbach 2015]

## Slide 31
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Neutral particle dissipation
Atomic physics does not scale with size – want greater access to the power channel.
Assume a single plasma scenario device, so that the baffle geometry can be optimized.
Needs study.

## Slide 32
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
(Divertor – H-mode jump start during plasma start-up)
(Power threshold is lower for shorter divertor legs, so easier access to D-T power.)

## Slide 33
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – “Rapid Strike-Point Replacement”
Thermal conductivity 5x higher than copper
Zero thermal expansion
Resistant to chemical erosion
Resistant to neutron damage
3D isotropic heat transport
Unparalleled thermal shock resistance
Minimal leading edges
Replacable
ANSYS: surface temperature
increase limited to 100 degrees – rather than mono-block failure
[M. van den Berg]

## Slide 34
HWU
MAST
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Diamond

## Slide 35
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Diamond

## Slide 36
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Divertor – Diamond
Joint aerospace-fusion development proposal to CNES in September, still alive.

## Slide 37
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Main wall – Main Chamber Recycling and Charge-eXchange (CX)
(ITER boundary plasma may be opaque to neutrals, so no core fueling from gas puffs.)
D0slow + D+fast  D+slow + D0fast
Charge-exchange (CX):
EIRENE neutral transport code (divertor sources off)
[D. Reiter, FZJ]

## Slide 38
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Main wall – Erosion from CX
For 300 eV T charge-exchange sputtering of walls | Pheat [MW] | annual run time [s/year] | beryllium net wall erosion rate [kg/yr] | boron net wall erosion rate [kg/yr] | carbon net wall erosion rate [kg/yr] | tungsten net wall erosion rate [kg/yr]
DIII-D | 20 | 104 | 0.13 | 0.11 | 0.08 | 0.16
JT-60SA | 34 | 104 | 0.22 | 0.19 | 0.15 | 0.27
EAST | 24 | 105 | 1.6 | 1.2 | 0.82 | 1.8
ITER | 100 | 106 | 77 [29] | 64 | 44 [53] | 92 [41]
FDF | 100 | 107 | 610 | 500 | 340 | 740
Reactor | 400 | 2.5x107 | 6500 | 5300 | 3700 | 7900 [5000]
A Kukushkin. B2-EIRENE calculation.
K Lackner. EU EFP Workshop on W. Velence, Hungary, Dec 7-9 2009.
MAIN WALL CHARGE-EXCHANGE EROSION [Stangeby, ARIES Town Meeting 2010]
“Have we been worrying about the wrong problem?” – P. C. Stangeby
Replace the wall regularly? No. Need to control main chamber CX erosion.

## Slide 39
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Main wall – Remove the neutrals
…
with liquid lithium
Needs study.

## Slide 40
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Main wall – If the boundary is opaque to neutrals: “Gas wall”?
Increase CX, but cool the boundary plasma to stay below the sputtering threshold?
toroidal circumference at injection location
distance along the plasma facing wall
Needs study.

## Slide 41
…
Overview
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY

## Slide 42
PREFACE | ITER PFCs | HIGH-DUTY CYCLE | SUMMARY
Concluding remarks
There are issues to be resolved if electricity from fusion energy is to make it onto the grid – many are complex and required highly developed problem solving skills
Please think as broadly as possible, and beware of “idea inertia” and The System
ITER won’t be running for quite a while, but coming up with good designs for post-ITER machines requires a lot of thinking and experimentation now
It is likely that civil society will experience a high level of stress this century – sustainable baseload energy from fusion is needed sooner rather than later
Akers Doctrine: Look for friends, i.e. other R&D areas that share your problems
Gentle movement towards engineering physics is encouraged
Consider aiming for engineering guidance rather than prediction